Cherokee Nation Businesses is requesting bids for three concrete slabs:

# 2- Located at Will Rogers Downs, 20900 S. 4200 Rd, Claremore, OK.

# 1- Located at Cherokee Casino, 1621 W Ruth Ave, Sallisaw, OK.

Will Rogers Downs Specifications (each slab):

22’x67’, 30”turn down with 16”pad 10” o.c with #6 double matted re-bar reinforcement. Min 3500 psi mix.

Cherokee Casino-Sallisaw:

21’x57’, 30”turn down 16”slab 10” o.c with #6 double matted re-bar reinforcement. Min 3500 psi mix.

All slabs and foundations will require 12” of overexcavation. Replace removed soil with 12” compacted road base. All spoils to be removed from site and disposed of legally.

All concrete waste must be disposed of off property; there is to be no concrete wash-out done on property.

Special Instructions for Will Rogers Downs:

Must obtain a license from the Oklahoma Horse Racing Commission (www.ohrc.org/license.html). If proposing firm is not current or does not have an Oklahoma Horse Racing Commission License, Owner will reimburse Contractor for the actual license fees.

All concrete waste must be disposed of off property; there is to be no concrete wash-out done on property.

Other:

The attached concrete and foundation sheet shall be used as the design basis for:

- Concrete details.

- Material details.

- Reinforcement details.

- Foundation details.

- Slab details.

Plan view dimensions for the slabs shall be as noted above.